## Slide 1: Three component model for the rheology of soft glassy materials
Marco Caggioni, Julie Hipp, Will Hartt, Emilio Tozzi, Pat Spicer
- P&G
Veronique Trappe, Manon Marchand - University of Fribourg
Structurant volume fraction
Structurant interaction
“Colloidal gels”
“Critical gels”
“colloidal Glasses”
Trappe, Veronique, and Peter Sandkühler. "Colloidal gels—low-density disordered solid-like states." Current opinion in colloid & interface science 8.6 (2004): 494-500.

## Slide 2: Outiline
Predicting viscosity at high shear rate
Designing new products textures
Notes: In our role, we need to predict the rheological behavior of a wide range of complex fluids at a similarly wide range of shear rates (x to x). The products are constantly evolving to adapt to changing consumer demands.

## Slide 3: Predicting rheology at filling (~104 s-1)
Stress (Pa)
Shear rate (s-1)
Rotational rheometer
HB fit and extrapolation (95% CI)
Capillary 1
Capillary 2
Filling
condition
Measure rotational rheology
Fit to yield stress fluid model
Herschel-Bulkley:
3. Extrapolate to filling condition

## Slide 4: Three-component model
TC:
Elastic
Plastic
Viscous
= yield stress
= critical shear rate
= background viscosity
Caggioni, Trappe, Spicer J. Rheol. 64(2): 413-422, 2020
HB:
Casson:

## Slide 5: Predicting rheology at filling (~104 s-1)
Shear rate (s-1)
Stress (Pa)
Rotational rheometer
TC fit and extrapolation (95% CI)
Capillary 1
Capillary 2
How did we miss this?
The model systems may have biased the model

## Slide 6: Model System: propylene glycol + carbopol
Benefits:
Commercially available ingredients
Simple preparation
Low solvent volatility
Robust to applied shear and age (degrades > 1000 Pa)
High viscosity of propylene glycol ( = 0.1 Pa.s)
Mixing with pitch blade impeller at 200 rpm
Notes: We prepare a microgel suspension of 2% Carbopol (974P NF) and (Ultrez) w/w in Propylen glycol. To prepare the sample we add 20g of carbopol to 1980g of Propylen glycol while mixing with a pitched blade impeller at ~200 rpm. We allow the sample to equilibrate for 24 to 48 h at room temperature continuing mixing at ~200 rpm.

## Slide 7: It’s like a simulation!
~20h

## Slide 8: Reproducible steady shear rheology

## Slide 9: Comparing model fits
Three-component model
= 17.0 Pa
= 0.42 s-1
= 0.27 Pa.s
= 0.99
Herschel-Bulkley model
= 24.2 Pa
k = 19.9 sn
n = 0.58
= 18.7

## Slide 10: Extrapolation to high shear rates
HB underpredicts
TC closer

## Slide 11: 3 scaling better than 2
Elastic
Plastic
Viscous
Shifts to higher , more challenging to measure as ↓

## Slide 12: Designing product texture
Olay “Butter”
Olay “Whip”
Olay “Cream”

## Slide 13
Designing new products textures
Tune solvent viscosity
Tune volume fraction

## Slide 14
2% Carbopol 974 in PG @ 25C
2% Carbopol Ultrez21 in PG @ 25C
K=0.005
K=0.045

## Slide 15
Connecting flow and oscillatory data
Casson would become TC model with 25% critical strain
Casson:
Seth, Jyoti R., et al. "A micromechanical model to predict the flow of soft particle glasses." Nature materials 10.11 (2011): 838-843.

## Slide 16: Summary
Describing flow curve with 3 regimes seems better than with 2
  The water based Carbopol model system may have biased the model development
TC model provides intuitive connection between parameters and microstructure
  Provides insight on how to tune material properties
We observe an interesting connection between yield strain and flow properties
  Work in progress