## Slide 1: Samples presentation
0.5 wt.% of carbopol SF2
in water
1.9 wt.% of carbopol 972p
in propylenglycol
6 wt.% of pnipam
synthetized with SDS
in propylenglycol
Solvents
high dependency of viscosity
with temperature for propylenglycol,
less blatant for water

## Slide 2: Light scattering
pnipam
synthetized with SDS
in propylenglycol
Guinier fit because they are small
T = 20°C
50°C
20°C
carbopol 972p
in propylenglycol
faint bump corresponds to
Rg ~ 340nm for both temperatures
carbopol SF2
in water
to be done (lots of
dust in samples from
Milan)
(sample diluted 2x since last
measurements, same shape)
sphere form factor

## Slide 3: Raw data of flow curves
carbopol 972p
in propylenglycol
carbopol SF2
in water
pnipam
synthetized with SDS
in propylenglycol

## Slide 4: Temperature effect Critical strains from amplitude sweeps and from TC fit
3 different samples, evolution with temperature
critical strain is constant but has three different definitions that don’t seem equivalent for all microgels

## Slide 5: Temperature effect dynamic yield stress from TC fit
temperature does not impact yield stress

## Slide 6: Temperature effect viscosities
on top: eta infinity extracted from TC fit
is the same for two different microgels !
at bottom: eta infinity scales linearly with
the viscosity from literature for two solvents

## Slide 7: Temperature effect on caracteristic shear rate

## Slide 8
yield stress here,
sorry Marco for the french
name in my code
Scatter matrix for TC model
in water
in propylenglycol
in propylenglycol

## Slide 9: Temperature effect on elastic modulus
small effect, unclear tendency